## Slide 1: Organic semiconductors Solar Cells & Light Emitting Diodes
Lior Tzabari, Dan Mendels, Nir Tessler
Nanoelectronic center, EE Dept., Technion

## Slide 2: Outline
Macroscopic View of recombination P3HT:PCBM
or – Exciton Annihilation as the bimolecular loss
Microscopic description of transport
  Implications for recombination

## Slide 3
What about recombination in P3HT-PCBM Devices
Let’s take a macroscopic look and decide on the relevant processes.
Picture taken from:
http://blog.disorderedmatter.eu/2008/06/05/picture-story-how-do-organic-solar-cells-function/ (Carsten Deibel)

## Slide 4: The Tool/Method to be Used
N. Tessler and N. Rappaport, Journal of Applied Physics, vol. 96, pp. 1083-1087, 2004.
N. Rappaport, et. al., Journal of Applied Physics, vol. 98, p. 033714, 2005.
Charge generation rate
Photo-current
Langevin recombination-current
No re-injection
QE as a function of excitation power
Signature of Loss
due to
Langevin Recombination

## Slide 5
What can we learn using simple measurements
(intensity dependence of the cell efficiency)
L. Tzabari, and N. Tessler, Journal of Applied Physics 109, 064501 (2011)
SRH (trap assisted)
Nt – Density of traps.
dEt - Trap depth with respect to the mid-gap level.
Cn- Capture coefficient
LUMO
HOMO
Mid
gap
dEt
Bimolecular
Monomol
P doped  Traps already with holes
Intrinsic (traps are empty)

## Slide 6
What can we learn using simple measurements
(intensity dependence of the cell efficiency)
Bi- Molecular
L. Tzabari, and N. Tessler, Journal of Applied Physics 109, 064501 (2011)
SRH (trap assisted)

## Slide 7: Recombination in P3HT-PCBM
4min | 
1.5e-12 | Kb[cm3/sec]
10
-2
10
0
10
2
0.55
0.6
0.65
0.7
0.75
0.8
0.85
0.9
0.95
1
4 min
Anneal
, - Experiment
, - Model
Intensity [mW/cm2]
Normalized QE
Kb – Langevin bimolecular
recombination coefficient
In practice detach it from its physical origin and use it as an independent fitting parameter
190nm of P3HT(Reike):PCBM (Nano-C)(1:1 ratio, 20mg/ml) in DCB
PCE ~ 2%
Notes: צריך קבוע יותר גדול – הגיוני כי הניידות גדלה.
אבל!!! מצד שני שינוי הניידות בלבד יביא לתוצאות הפוכות מאחר והגדלת הניידות מגדילה גם את יכולת האיסוף – וברגע שיכולת האיסוף גדלה כמות נושאי המטען האפקטיבית בהתקן קטנה ומנגנוני האיבוד נכנסים מאוחר יותר.
=> יכול להיות שינוי תלוי מורפולוגיה בלבד.

## Slide 8: Recombination in P3HT-PCBM
10min | 4min | 
8e-12 | 1.5e-12 | Kb[cm3/sec]
4 min
10 min
, - Experiment
, - Model
Notes: צריך קבוע יותר גדול – הגיוני כי הניידות גדלה.
אבל!!! מצד שני שינוי הניידות בלבד יביא לתוצאות הפוכות מאחר והגדלת הניידות מגדילה גם את יכולת האיסוף – וברגע שיכולת האיסוף גדלה כמות נושאי המטען האפקטיבית בהתקן קטנה ומנגנוני האיבוד נכנסים מאוחר יותר.
=> יכול להיות שינוי תלוי מורפולוגיה בלבד.

## Slide 9
Shockley-Read-Hall Recombination
LUMO
HOMO
Mid gap
, - Experiment
, - Model
4 min
10 min
L. Tzabari and N. Tessler, "JAP, vol. 109, p. 064501, 2011.
dEt
Intrinsic (traps are empty)
I. Ravia and N. Tessler, JAPh, vol. 111, pp. 104510-7, 2012. (P doping < 1012cm-3)

## Slide 10
Shockley-Read-Hall + Langevin
10min | 4min | 
1.2e17 | 1.9e17 | Nt [1/cm3]
0.371 | 0.435 | dEt [eV]
0.5e-12 | 0.5e-12 | Kb[cm3/sec]
4 min
10 min
, - Experiment
, - Model
LUMO
HOMO
Mid
gap
dEt
The dynamics of recombination at the interface is both
SRH and Langevin

## Slide 11
Exciton Polaron Recombination
M. Pope and C. E. Swenberg, Electronic Processes in Organic Crystals., 1982.
A. J. Ferguson, et. al., J Phys Chem C, vol. 112, pp. 9865-9871, 2008 (Kep=3e-8)
J. M. Hodgkiss, et. al., Advanced Functional Materials, vol. 22, p. 1567, 2012. (Kep=1e-8)
Neutrally excited molecule (exciton) may transfer its energy to a charged molecule (electron, hole, ion).
As in any energy transfer it requires overlap between the exciton emission spectrum and the “ion” absorption spectrum.

## Slide 12
Exciton Polaron Recombination
Nt – Density of traps.
dEt - trap depth with respect to the mid-gap level.
Kep – Exciton polaron recombination rate.
Kd– dissociation rate 1e9-1e10 [1/sec]
Sensitivity | 10min | 4min | 
0 | 1.05e17 | 1.9e17 | Nt [1/cm^3]
0.015 | 0.365 | 0.435 | dEt [eV]
1.08e-8 | 1.6e-8 | 1.6e-8 | Kep[cm^3/sec]
4 minutes
10 minutes
, - Experiment
, - Model
A. J. Ferguson, et. al., J Phys Chem C, vol. 112, pp. 9865-9871, 2008 (Kep=3e-8)
J. M. Hodgkiss, et. al., Advanced Functional Materials, vol. 22, p. 1567, 2012. (Kep=1e-8)

## Slide 13
T. A. Clarke, M. Ballantyne, J. Nelson, D. D. C. Bradley, and J. R. Durrant, "Free Energy Control of Charge Photogeneration in Polythiophene/Fullerene Solar Cells: The Influence of Thermal Annealing on P3HT/PCBM Blends," Advanced Functional Materials, vol. 18, pp. 4029-4035, 2008. (~50meV stabilization)
4 minutes
10 minutes
Sensitivity | 10min | 4min | 
0 | 1.05e17 | 1.9e17 | Nt [1/cm^3]
0.015 | 0.365 | 0.435 | dEt [eV]
1.08e-8 | 1.6e-8 | 1.6e-8 | Kep[cm^3/sec]
Traps or CT states are stabilized during annealing

## Slide 14
Bias Dependence
10 minutes anneal

## Slide 15
Charge recombination is activated

## Slide 16
Obviously we need to understand better the recombination reactions
Let’s look at the Transport leading to…

## Slide 17: Electronic Disorder
E
x
E
Density of states
Band
Tail states (traps)
E
Density of states
Density of localized states
High Order
E
x
Low disorder
E
x
High disorder
E
Band
Density of states
Modeling Solar Cells based on material with

## Slide 18
Disordered hopping systems
are
degenerate semiconductors
Y. Roichman and N. Tessler, APL, vol. 80, pp. 1948-1950, Mar 18 2002.
White Dwarf
The notion of degeneracy or degenerate gas is not unique to semiconductors.
Actually it has its roots in very basic thermodynamics texts.
To describe the charge density/population one should use
Fermi-Dirac statistics and not Boltzmann

## Slide 19
Degenerate Gas
White Dwarf
When the Gas is non-degenerate the average energy of the particles is independent of their density.
When the Gas is degenerate the average energy of the particles depends on their density.
Enhancing the density of a degenerate electron gas requires substantial energy (to elevate the average energy/velocity)
 this stops white dwarfs from collapsing (degeneracy pressure)

## Slide 20
Degenerate Gas
White Dwarf
Enhancing the density of a degenerate electron gas requires substantial energy (to elevate the average energy/velocity)
Relation to Semiconductors
The simplest way:
Enhanced random velocity = Enhanced Diffusion
(Generalized Einstein Relation)
But what about localized systems?
Can we relate enhanced average energy to enhanced velocity?
Wetzelaer et. al., PRL, 2011
GER Not Valid

## Slide 21
Monte-Carlo simulation of transport
G.E.R.
Monte-Carlo
Standard M.C. means uniform density
Y. Roichman and N. Tessler, "Generalized Einstein relation for disordered semiconductors - Implications for device performance," APL, 80, 1948, 2002.

## Slide 22: Comparing Monte-Carlo to Drift-Diffusion & Generalized Einstein Relation
qE
qE
Implement contacts as in real Devices
GER Holds for real device Monte-Carlo Simulation

## Slide 23: Where does most of the confusion come from
J. Bisquert, Physical Chemistry Chemical Physics, vol. 10, pp. 3175-3194, 2008.
D The intuitive Random Walk
The coefficient describing
Generalized Einstein Relation is defined ONLY for

## Slide 24: What is Hiding behind
E
X
E
X
Charges move from high density region to low density region
Charges with High Energy move from high density region to low density
There is an Energy Transport

## Slide 25
Degenerate Gas
White Dwarf
Enhancing the density of a degenerate electron gas requires substantial energy (to elevate the average energy/velocity)
Relation to Semiconductors
The fundamental way:
Density Energy Density Gradient Energy Gradient
Driving Force
Enhanced “Diffusion”

## Slide 26
All this work just to show that the Generalized Einstein Relation
Is here to stay?!
Enhanced “Diffusion”
There is transport of energy even in the absence of Temperature gradients
degenerate
is
There is an energy associated with the charge ensemble
And we can both quantify and monitor it!
D. Mendels and N. Tessler, The Journal of Physical Chemistry C, vol. 117, p 3287, 2013.

## Slide 27
s=78meV (3kT)
DOS = 1021cm-3
N=5x1017cm-3=5x10-4 DOS
Low Electric Field
B. Hartenstein and H. Bassler, Journal of Non - Crystalline Solids 190, 112 (1995).
How much “Excess” energy is there?
150meV
EF

## Slide 28
There is an Energy associated with the charge ensemble
And we can both quantify and monitor it!
We should treat the relevant reactions by considering the
Ensembles’ Energy
Transport
&
Recombination
are reactions
Ensembles’ Energy
D. Mendels and N. Tessler, The Journal of Physical Chemistry C, vol. 117, p 3287, 2013.

## Slide 29
e
Center of Carrier Distribution
Mobile Carriers
Density Of States
Charge Distribution
Think Ensemble
The Single Carrier Picture
D. Monroe, "Hopping in Exponential Band Tails," Phys. Rev. Lett., vol. 54, pp. 146-149, 1985.

## Slide 30
Think Ensemble
e
Center of Carrier Distribution
Mobile Carriers
1) This is similar to the case of a band with trap states
2) There is an extra energy available for recombination.
Mathematically, the “activation” associated with this energy is already embedded in the charge mobility

## Slide 31
The operation of Solar Cells is all about balancing nergy
Think “high density” or “many charges” NOT “single charge”
There is extra energy embedded in the ensemble
(CT is not necessarily bound!)

## Slide 32: The High Density Picture Mobile and Immobile Carriers
Mobile Carriers
s=3kT
DOS = 1021cm-3
N=5x1017cm-3=5x10-4 DOS
Low Electric Field
Transport is carried by high energy carriers
Is it a BAND?
Jumps distribution
EF

## Slide 33
Summary
The Generalized Einstein Relation is rooted in basic thermodynamics
Holds also for hopping systems
Think Ensemble
Energy transport (unify transport with Seebeck effect)
There is “extra” energy in disordered system [0.15 – 0.3eV]
Is this important in/for P3HT:PCBM based solar cells (probably)
Langevin is less physically justified compared to SRH
At the high excitation regime:
Polaron induced exciton annihilation is the bimolecular loss
Why some systems exhibit Langevin and some not?
Why some exhibit bi-molecular recombination?
Why some exhibit polaron induced exciton quenching

## Slide 34: Thank You
Israeli Nanothecnology Focal Technology Area on "Nanophotonics for Detection"
Ministry of Science, Tashtiyot program
Helmsley project on Alternative Energy of the Technion, Israel Institute of Technology, and the Weizmann Institute of Science

## Slide 36: Original Motivation
Measure Diodes I-V
Extract the ideality factor
The ideality factor
Is the Generalized Einstein Relation
The Generalized Einstein Relation is NOT valid for
organic semiconductors
Y. Vaynzof et. al. JAP, vol. 106, p. 6, Oct 2009.
G. A. H. Wetzelaer, et. al., "Validity of the Einstein Relation in Disordered Organic Semiconductors," PRL, 107, p. 066605, 2011.

## Slide 37
Chart: 
| 0 | 0.25
Cathode | -4 | -4
Anode | -4 | -4
vacuum | 0 | 0
vacuum | 0 | 0
dipole 1 | 0 | 0
dipole 2 | 0 | 0
LUMO of PCBM
HOMO of P3HT
How do they work?
P3HT
Acceptor
Donor
PCBM
Immediately after illumination

## Slide 38
How do they work?
P3HT
Acceptor
Donor
PCBM
LUMO of PCBM
HOMO of P3HT
Chart: 
| 0 | 0.25
Cathode | -4 | -4
Anode | -4 | -4
vacuum | 0 | 0
vacuum | 0 | 0
dipole 1 | 0 | 0
dipole 2 | 0 | 0